TECHNICAL DATA SHEET

LA VIA LATTEA

sez. 1.0 Technical characteristics

La Via Lattea is a decorative paint with iridescent effects. Thanks to the flakes of silver mother-of-pearl, the applied product reacts to light, changing its reflections according to the different lighting, in light colours. This product affords good washability, is anti-bacterial and makes for countless application possibilities.

sez. 2.0 Use

La Via Lattea is suitable for decorating indoor wall surfaces.

sez. 3.0 Preparing the surface

Preparing the wall is vital to the success of the coating. It is therefore advisable to trim and insulate properly before use, and to apply Primus Sabbia (as specified in the application method), which guarantee optimal grip and absorbency of the product.

sez. 4.0 Application method

La Via Lattea is not ready for use. Introduce the quantity of COLOURING AGENT specified in the catalogue and then add water (300 ml of water each liter of La Via Lattea). Mix well until the shade obtained is completely even. Before applying the product, it’s necessary to apply our Primus Sabbia (ready to use) to prepare the wall. Afterwards, the product can be applied in 2 coats with a brush, with irregular movements, with light pressure, so as not to see the brushstrokes. The average coverage of the product is 5/6 m² each liter.

sez. 5 Protective Finish

The product has a good washability, with non aggressive soaps. Anyway it can be protected with: Vetro: applied by roller, dilution is not necessary. It affords good coverage, water-resistance and complete washability of the wall.

sez. 6.0 Technical characteristics: application

| Dilution/Mixing | 300 ml of water in each liter of VIA LATTEA |
| --- | --- |
| Consumption | 200 g/m² |
| Tools for application | Brush |
| Primus | Primus Sabbia |
| Protective coating | Vetro |
| Application temperature | The ambient temperature must not be less than +5° C. Do not apply onto hot surfaces or those exposed to sunlight. |
| Drying time | The drying time varies between 6 and 8 hours |

sez. 7.0 Caratteristiche tecniche: il prodotto

| Composition | Water, additives, mother-of-pearl flakes. |
| --- | --- |
| Specific weight | 1.23 Kg/l |
| pH after 30 days | > 8-8.5 |
| Viscosity | > between 10000 and 12000 cps (Brookfield) |
| Storage temperature | Store in a sealed pot at a temperature of more than +5° C. Keep away from extreme cold. |
| EU VOC limit value for this product (cat. A/I): 300 g/l (2007) 200 g/l (2010) | Max content VOC 44 g/l |
| Colours available | As per our catalogue |
| Pot sizes | Lt 1 – 2,5 – 5 |
| Warnings | If inhaled: Take the patient to a well ventilated location. Contact with eyes: rinse immediately with plenty of running water for at least 10 minutes. Skin contact: wash with running water; avoid prolonged contact. |

sez. 8.0 Toxicological data

The material is not labelled as irritating. There are no known effects on the eyes and skin.